STUDY OF CREEP OF ALUMINA-FORMING AUSTENITIC STAINLESS STEEL FOR HIGH-TEMPERATURE ENERGY APPLICATIONS
A Thesis
Submitted to the Faculty
in partial fulfillment of the requirements for the
degree of
Master of Science
by
Natalie Petrovna Afonina
Thayer School of Engineering
Dartmouth College
Hanover, New Hampshire
June 2016
Examining Committee:
Chairman_______________________
(Dr. Ian Baker)

        Member________________________
(Dr. Rachel Obbard)

Member________________________
(Dr. Abc Abc)

___________________
F. Jon Kull
Dean of Graduate Studies

Thayer School of Engineering
Dartmouth College

“Study of creep of alumina-forming austenitic stainless
steel for high-temperature energy applications”

Natalie Petrovna Afonina
Master of Science

Dr. Ian Baker
Dr. Rachel Obbard
Dr. Abc Abc
ABSTRACT
General intro…. The microstructure of a high-temperature superalloy was examined before and after creep and heat treatments. It was determined that…
Comparison between….show that….Abc…. Application of this work in future studies could reduce noise, improve abc and reduce abc.
A constant stress creep machine was designed and constructed, since it was necessary to hold stress constant in the study. Bamboo structured and coarse-grain polycrystalline specimens were fabricated
with varying large grain sizes. Creep tests were conducted holding stress and temperature constant while monitoring strain rate.

Alloyed with aluminum to provide corrosion resistance, alumina-forming austenitic (AFA) stainless steels have shown promise for application in the harsh environments seen in energy production where strong materials that are oxidation and corrosion resistant are needed. The role of precipitates in AFA-type alloys, Fe-20Cr-30Ni-2Nb-5Al and DAFA26 was investigated in this study.
        The effects of cold work on the microstructural evolution during aging of solutionized Fe-20Cr-30Ni-2Nb-5Al (at. %), was investigated. Cold work prior to aging at either 700°C or 800°C facilitated the heterogeneous precipitation of both Laves phase and B2-type NiAl precipitates. While often co-located after cold work, these particles were distinct. γ’-Ni3Al precipitates were also observed in samples aged at 700°C with 90% prior cold work. Compared to material that had not been strained, defects introduced by 50 and 90% cold work at 700°C and 90% cold work at 800°C not only caused a more rapid precipitation in the matrix but also an increase in the total volume fraction of precipitates as compared to material that had been simply aged.
The effect of aging on the microstructure and mechanical properties of Fe-20Cr-30Ni-2Nb-5Al (at. %) was evaluated. An increase in the volume fraction of B2 and Laves phase precipitates in the alloy was accompanied by an increase in the yield strength from 205 MPa after the solutionizing anneal up to 383 MPa after aging at 800°C for 1325 h. After aging for 1325 h, even with extensive intermetallic grain boundary coverage, the alloy showed a room temperature elongation of 19%.
The relationship between the crystallographic orientation of Laves Fe2Nb and B2-NiAl precipitates and their f.c.c. parent matrix was investigated. Four variants of the m // p, m // p orientation relationship proposed by Denham and Silcock (J. Iron Steel Inst. 207 (1969) 582) were observed for the Laves phase, and six variants of the m // p, m // p Kurdjumov-Sachs relationship were observed for the B2-NiAl phase.
The microstructural evolution of DAFA26 was also observed. In addition to Laves phase and B2-NiAl precipitates, the evolution of the Ni3Al precipitates present in this alloy was investigated.

ACKNOWLEDGEMENTS

First, I would like to thank my adviser Dr. Ian Baker, whose patience, expertise, unwavering support and encouragement made it possible for me to complete my studies. I would also like to extend my thanks to those who offered guidance and support over the years: the Baker Research Group, Dr. Geneva Trotter, Mr. Kevin Hammonds, Hailey Nicholson and Dr. Daniel Cullen. The Carpenter Technology Corporation for providing the alloy for this study. The Thayer School of Engineering Instrument Room staff for teaching me how to wire electronics properly and avoid shocking myself.
Claire Stolz, for the pep talks that could rouse armies and accompanying me on moonlit walks at the Methow. I’m sure without you by my side the cougars would have gotten me.
Nate Beatty, for being there in the darkest hour, for sharing a love of mini-adventures and having my back when I’m in places like Yemen or Tajikistan.
Mark Fischer, for being a watchful older brother and lending a new perspective. You’ve kept me successfully out of trouble most of the time.
Julian Childs-Walker, for being my twin and remaining the only person to ever hitchhike beyond the Arctic Circle to go on an adventure with me. You’ve continuously helped me get up to no good and our conversations help me make sense of this world.
I can’t convey how much I owe my family for getting me this far. Without you I would be nothing.
My sister Jane Bellousov for being the level-headed one in the family and looking up to me even when I screw up. I can’t wait to go on more adventure trips with you.
My father Yevgeniy Belousov, for encouraging me to stop working so hard and go on more climbing breaks outside. You’ve provided much needed perspective and inspiration.
My grandmother Dr. Galina Gataulina who worries for me about having time to finish my Masters degree, encouraging me to not procrastinate and feeding me delicious piroshki.
My grandfather Dr. Akhiyar Myginovich for reminding me that life can be filled with meaningful work and to never lose your inner child. For always being proud and supportive and teaching me how to use a crowbar to pull nails and lay bricks in a straight line. I wish you’d still be here to see me defend my thesis.
Most importantly, I dedicate this thesis to my mother, Dr. Irina Afonina, without whom I would not be here today. Who through her sacrifices supported me at every step from the moment when just the two of us immigrated to the United States from Russia and gave me room to figure things out on my own and spread my wings. You sadly left us before I could finish this thesis, but I know you would’ve been proud of me.

I dedicate this thesis to my mother.
Your support, unconditional love and sacrifices are responsible for everything I’ve accomplished.
 I miss you every day.
LIST OF TABLES
Table 1: Summary of firn air sampling sites and characteristics (Buizert, 2013) .............15
Table 2: Permeability results from testing the wedged membrane holder .......................32

LIST OF FIGURES
Figure 1: Mechanisms leading to sintering in polar firn (Buizert, 2013) .....................15
Figure 2: Calibration results for permeameter models...................................................27

CHAPTER 1	INTRODUCTION
Paragraph 1: General information about energy applications, creep, superalloys, microstructure.
Paragraph 2: More in depth information. …….Due to this lack of knowledge, these are the implications….. In order to do “blank”, the role and mechanism of creep in these superalloys must be better understood.
Paragraph 3: This thesis focuses on the process…..This superalloy was chosen because…. These heat treatments and temperatures and tensions were chosen because…. The following measurements were done in conjunction with scanning electron microscopy to better understand the relationship between grain size…..The overarching goals of this thesis are to:

1.	Characterize some stuff
2.	Understand some stuff
3.	Do more
4.	Do more

abc

CHAPTER 2	BACKGROUND
2.1	Alumina Forming Austenitic Stainless Steels
2.1.1	Small Specific Metal Thing
Paragraph 1
Paragraph 2

2.1.2
Paragraph 1
Paragraph 2

2.1.3	And Yet Another
Paragraph 1
Paragraph 2

2.2	Overview of Steady State Creep
Paragraph 1
Paragraph 2

2.3	Outline of Research Project
The purpose of this thesis is to investigate the creep rate and mechanical properties of an alumina forming austenitic stainless steel, specifically the model alloy Fe-20Cr-30Ni-2Nb-5Al, for different heat treatment conditions.
The investigation proceeds as follows:
 A constant stress creep apparatus was designed and built.
Samples were prepared by machining and then heat treated at different conditions
Constant stress creep tests were run for each sample.
The microstructure was examined before and after creep testing was complete using scanning electron microscopy.
Strain rate jump tests were conducted on specimens under a variety of heat treatment conditions.
 Chapter 3 covers materials preparation, the design, construction and testing of a constant stress creep apparatus, and materials characterization techniques.
Chapter 4 details the microstructure changes and precipitate evolution in Fe-20Cr-30Ni-2Nb-5Al before, during and after constant stress creep testing.
Chapter 5 discusses the effect of different heat treatment conditions on mechanical properties.

In Chapter 6, the conclusions of this research project are summarized.
Chapter 7 suggests future work.
CHAPTER 3	EXPERIMENTAL METHODS

3.1	Materials Preparation

3.1.1	Materials Used
The alloy Fe-20Cr-30Ni-2Nb-5Al was used for both the creep and strain-rate jump tests throughout this study. The alloy was provided by Carpenter Technology Corporation (Wyomissing, PA). A split-cast vacuum induction melting heat was used to cast the alloy into tapered ingots. The ingots were then press forged into rectangular bars with the following dimensions: 0.625” x 0.75’’ x 24’’. The chemical composition of the alloy was analyzed by LECO combustion analysis and X-ray Fluorescence. Table 3.1 compares the analyzed element compositions with the theoretically calculated weight percent ratios.
Table 3.1 Chemical composition comparison of the alloy
Element Analyzed	Theoretical (wt%)	Analyzed (wt%)
Nickel	31.88	31.90
Chromium	18.83	18.98
Niobium	3.36	3.34
Aluminum	2.44	2.48
Carbon	0.00	0.02
Cobalt	0.00	0.01
Copper	0.00	<0.01
Manganese	0.00	<0.01
Molybdenum	0.00	0.01
Phosphorus	0.00	<0.005
Silicon	0.00	<0.01
Sulfur	0.00	<0.001

3.1.2	Sample Machining
In preparation for both creep testing and strain-rate jump tests, the alloyed material was machine milled and then sectioned with a saw. The TRAK DPM SX3P bed mill with a 40 taper spindle and ProtoTRAK SMX control was used with zinc-coated carbide end mills to mill the specimens into the T-bone shapes necessary to attach to the grips of the creep testing and strain-rate jump testing apparatuses. To ensure the accurate geometry of each T-bone, the specimen was sectioned using coolant with a Model 650 Low Speed Diamond Wheel Saw from South Bay Technology, Inc.

Figure 3.1: CAD file drawing of a T-bone sample fitted into one side of the creep machine’s grips.

3.1.3	Material Homogenization and Heat Treatments
For all tests in this study, the as-cast model alloy was homogenized for 4 hours at 1250ºC in a vacuum and then water-quenched. This temperature and time was chosen with consideration to prior work with Fe-20Cr-30Ni-2Nb-5Al, where it was determined that a solutionized single phase γ-matrix could be consistently formed. This was confirmed with SEM images of the as-cast raw material and compared with the material after a heat treatment homogenization conducted at 1250ºC for 4 hours.
All solutionizing heat treatments were conducted using a Thermo Scientific Type 54233 Lindberg Closed-Shell tube furnace. Specimens were placed on top of a piece of alumina and maneuvered to the center of the furnace tube with a rod. The furnace tube was then vented with argon and placed under a pressure of 0.01 MPa to maintain an oxygen-free environment and to prevent oxidation of the sample inside the furnace until the heat treatment was complete. Once the sample was sealed inside the furnace, the furnace was turned on and the temperature set to 1250ºC. When the solutionizing anneal was complete, the pressure seal was broken and the sample rapidly quenched in water with a substantially greater mass compared to the sample.
All heat treatments of the samples after they were homogenized were conducted at 800ºC for a variety of time intervals ranging from 0 to 240 hours. Heat treatments were conducted in a Barnstead Thermolyne Type 47900 Furnace. Samples were placed inside an alumina crucible and then positioned at the center of the furnace for the duration of the heat treatment. At the completion of the heat treatment, the samples were quenched with water.

3.2	Constant Stress Creep Apparatus Design and Testing

3.2.1	Overview of Constant Stress Creep Testing Machines
Creep measurements were made using the methods developed by Garofalo 1962{ | Garofalo, et al., 1962 | | |zu:2902168:5TKQ6V7D} and used for example in…./ Using a custom apparatus that had been verified…. Before measurements were taken the creep testing machine was calibrated using…. Samples until the measured stress and strain was within the bounds of literature values. This many measurements were done at these parameters.

3.2.2	Design of Creep Test Apparatus
Calibration was done on the built creep machine through ….
Abc

3.2.3	Calibration of Apparatus
Calibration was done on the built creep machine through ….
Abc

3.2.4	Specimen Preparation
 Tensile test specimens were milled to dog-bone geometry with a gauge length of 10 mm, width of 2.65 mm, thickness of 0.8 mm, and polished to a mirror finish using 800 grit silicon carbide papers followed by 0.3 μm alumina powder.

3.2.5	Testing and Operation Procedures
Abc

3.3	Materials Characterization
3.3.1	Scanning Electron Microscopy
In preparation for imaging with the Scanning Electron Microscope (SEM), samples were compression mounted and polished on a turntable using successively finer silicon carbide sandpaper, then with 0.3µm followed by a finer 0.05µm alumina powder dissolved in water. Samples were placed on a polishing vibrometer with liquid metal polish for ~3 hours to achieve a mirror finish.
Samples were imaged using a Tescan Vega3 SEM outfitted with Bruker Quantax Energy-dispersive X-ray Spectroscopy (EDS) and electron backscatter diffraction (EBSD) detectors. Samples were imaged using back-scattered electrons (BSE) with a working distance of ~10mm and operating voltage of 15 keV.

3.3.2	Strain Rate Jump Testing
  Tensile test specimens were milled to dog-bone geometry with a gauge length of 10 mm, width of 2.65 mm, thickness of 0.8 mm, and polished to a mirror finish using 800 grit silicon carbide papers followed by 0.3 μm alumina powder.
        After thermo-mechanical processing, room temperature tensile tests w

CHAPTER 4	EFFECT OF HEAT TREATMENT CONDITIONS ON CONSTANT STRESS CREEP RATES AND MICROSTRUCTURE

4.1	Effect of Heat Treatment Conditions on Microstructure
4.1.1	Experimental
Abc
Abc

4.1.2	Results and Discussion
Abc

4.2	Effect of Heat Treatment Conditions on Constant Stress Creep Rates
4.2.1	Experimental
Abc Tensile test specimens were milled to dog-bone geometry with a gauge length of 10 mm, width of 2.65 mm, thickness of 0.8 mm, and polished to a mirror finish using 800 grit silicon carbide papers followed by 0.3 μm alumina powder.
Abc

4.2.2	Results and Discussion
Abc
Abc

4.3	Effect of Constant Stress Creep Testing on Microstructure
4.3.1	Results and Discussion
Abc
Abc

4.3.2	Subsection 2
Abc
Abc

CHAPTER 5	EFFECT OF HEAT TREATMENT CONDITIONS ON MECHANICAL PROPERTIES

5.1	Experimental

5.1.1	Sample Preparation
Abc
Abc

5.1.2	Strain rate jump testing experimental setup
Abc
Abc

5.2	Results and Discussion
5.2.1	Mechanical Properties of Heat Treated Specimens
Abc
Abc

5.3	Summary
Abc
Abc
CHAPTER 6	CONCLUSION

Paragraph 1
Paragraph 2
Paragraph 3
CHAPTER 7	FUTURE WORK

Future work should be divided into two main focus areas:

1.	Abc

2.	Abc
8	REFERENCES